 

American Marking Inc

2435 Vale Drive

Birmingham, Al 35244

Phone: (Tn): 423-843-0446 or (Al): 205-987-0151

Website: [www.americanmarking.com](http://www.americanmarking.com)

**Product Specification AERO 6330**

|  |  |
| --- | --- |
| IIMAK Product Category | Core Choice |
| General Description | General purpose, non-toxic invisible ink that fluoresces under ultraviolet (black) light. This air-dry, waterproof ink is commonly used for identification purposes at events. Imprint remains on skin for up to 24 hours. Designed to stay moist in pads and markers for extended life. |
| System | Solvent |
| Colors | Fluoresces Blue\*, Green, Red, YellowCustom Colors: Fluoresces Orange, Violet, Pink |
| Colorant | Dye - blue, green. Other colors are Pigment. |
| Surface Type | Skin, Non-Porous |
| Typical Substrates | Skin, plastic |
| Suggested Application Method | Hand stamp, Marker (GLO-PEN) |
| Regulatory / 3rd Party Specifications | REACH, HAPS Free |
| Dry Time | 15 seconds |
| Recommended Thinner / Reactivator | 6330 Solvent |
| Shelf Life | 12 months: Dye9 months: Pigment |
| Shipping Status | Flammable LiquidUPS ground surcharge applies on 1QT or larger container |
| \*Only Blue is truly “invisible.” Other colors may leave a visible stain. September 2013 |  |  |
|  |  |  |
|  |  |  |
|  |  |  |
|  |  |  |
|  |  |  |